

REACTIVE DYES VINYL SULPHONE BASE

|  |  |
| --- | --- |
| **Reactive Vinyl Sulphone Base Dye** | **FASTNESS PROPERTIES** |
| Light | Washing | Perspiration | Hypochlorite | Dischargeability |
| Reactive Red 4BReactive Red - 24 |   | 6 | 3-4 | 5 | 1 | G |
| Reactive Red 5BReactive Red - 35 |   | 6 | 3-4 | 5 | 1 | G |
| Reactive Red C2GReactive Red - 106 |   | 4 | 4-5 | 5 | 1 | G |
| Reactive Red RBReactive Red - 198 |   | 5-6 | 4-5 | 4 | 1 | F |
| Reactive Orange 3RReactive Orange - 16 |   | 5-6 | 5 | 5 | 1 | G |
| Reactive Orange 2RReactive Orange - 7 |   | 4-5 | 4-5 | 5 | 1-2 | G |
| Reactive G. Yellow RReactive Yellow - 20 |   | 5 | 4-5 | 5 | 1 | G |
| Reactive Yellow FGReactive Yellow 42 |   | 5 | 5 | 5 | 1 | G |
| Reactive Yellow GRReactive Yellow -15 |   | 6 | 5 | 5 | 1 | G |
| Reactive Yellow RTNReactive Yellow - 24 |   | 6-7 | 4 | 4 | 2 | F |
| Reactive G. Yellow RNLReactive G. Yellow - 107 |   | 5 | 4-5 | 4-5 | 1 | G |
| Reactive Yellow RReactive Yellow - 77 |   | 4-5 | 5 | 5 | 1 | G |
| Reactive Yellow GLReactive Yellow - 37 |   | 6-7 | 4-5 | 5 | 1 | G |
| Reactive Black BReactive Black -5 |   | 5 | 4-5 | 5 | 1 | G |
| Reactive Black RLReactive Black - 31 |   | 7 | 4-5 | 5 | 3-4 | F |
| Reactive Violet 5RReactive Violet - 5 |   | 6-7 | 4 | 3-4 | 5 | P |
| Reactive Tur. Blue G.Reactive Blue-21 |   | 6 | 4-5 | 5 | 3-4 | P |
| Reactive Tur. Blue H2GP  |   | 6 | 4 | 5 | 3-4 | P |
| Reactive Blue 3RReactive Blue - 28 |   | 7 | 4 | 5 | 3-4 | G |
| Reactive Blue RReactive Blue - 19 |   | 6-7 | 4-5 | 4-5 | 3-4 | F |
| Reactive Blue RGBReactive Blue - 250 |   | 4-5 | 3-4 | 4 | 1 | G |
| Reactive Blue BBReactive Blue - 220 |   | 6-7 | 4 | 5 | 1 | G |
| Reactive Dark Blue HRReactive Blue - 89 |   | 5-6 | 3-4 | 5 | 1 | F |
| Reactive Navy Blue GGReactive Blue - 203 |   | 4-5 | 3-4 | 5 | 1 | F |
| Reactive Navy Blue GG |   | - | - | - | - | - |
| Reactive Brown GRReactive Brown - 18 |   | 6 | 4-5 | 4 | 1 | G |
| Reactive Black WNN |   | 5 | 4-5 | 5 | 1 | G |