

RECATIVE COLD DYES

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| **Reactive Cold Dyes** | | **FASTNESS PROPERTIES** | | | | |
| Light | Washing | Perspiration | Hypochlorite | Dischargeability |
| Reactive Red M5B Reactive Red - 2 |  | 4-5 | 4-5 | 3-4 | 1 | P |
| Reactive Red M8B Reactive Red - 11 |  | 4-5 | 4-5 | 2 | 4 | P |
| Reactive Magenta MB Reactive Violet - 13 |  | 4-5 | 5 | 4-5 | 1 | F |
| Reactive Orange M2R Reactive Orange - 4 |  | 5 | 5 | 4 | 4 | P |
| Reactive Orange M2RJ |  | 3-4 | 4 | 4 | 4-5 | P |
| Reactive Gol. Yellow MR Reactive Yellow - 44 |  | 5 | 4-5 | 4 | 1 | P |
| Reactive Yellow MR EX H/C Reactive Yellow - 44 |  | 5 | 4-5 | 4 | 1 | P |
| Reactive Yellow M3R Reactive Yellow - 36 |  | 6 | 5 | 4 | 2 | G |
| Reactive Yellow M4R Reactive Orange - 14 |  | 5 | 4-5 | 4 | 1 | P |
| Reactive Yellow M8G Reactive Yellow - 86 |  | 6 | 4-5 | 4-5 | 1 | G |
| Reactive Yellow M4G Reactive Yellow - 22 |  | 6 | 4 | 5 | 1 | G |
| Reactive Yellow MGR Reactive Yellow - 7 |  | 6 | 5 | 4-5 | 4-5 | P |
| Reactive Violet C4R Reactive Violet - 12 |  | 4 | 3 | 4 | 1 | P |
| Reactive Violet C2R Reactive Violet - 14 |  | 3-4 | 3 | 4 | 1 | P |
| Reactive Blue MR Reactive Blue - 4 |  | 6 | 5 | 5 | 2 | P |
| Reactive Blue M2R Reactive Blue - 81 |  | 6 | 5 | 4-5 | 1 | P |
| Reactive Blue M2R H/C Reactive Blue - 81 |  | 6 | 5 | 4-5 | 1 | P |
| Reactive Navy Blue M3R Reactive Blue - 9 |  | 5 | 4-5 | 3 | 3 | P |
| Reactive Blue M4GD H/C Reactive Blue - 168 |  | 6 | 5 | 3-4 | 2 | P |
| Reactive Tur. Blue MGN Reactive Blue - 140 |  | 6 | 4 | 4 | 2-3 | P |
| Reactive Tur. Blue Ha5G Reactive Blue - 71 |  | 6 | 3-4 | 4-5 | 3-4 | P |