RECATIVE HOT DYES

|  |  |
| --- | --- |
| **Reactive Hot Dyes** | **FASTNESS PROPERTIES** |
| Light | Washing | Perspiration | Hypochlorite | Dischargeability |
| Reactive Yellow H7GLReactive Yellow - 57 |   | 6 | 5 | 5 | 2 | G |
| Reactive Yellow H4GReactive Yellow - 18 |   | 6 | 5 | 5 | 1 | G |
| Reactive Gol. Yellow HRReactive Yellow - 12 |   | 6 | 5 | 5 | 3 | F |
| Reactive Orange H2RReactive Orange - 13 |   | 4 | 5 | 4 | 4 | P |
| Reactive Red H8BReactive Red - 31 |   | 4 | 4 | 4 | 3 | P |
| Reactive Red 6BXReactive Red - 76 |   | 4 | 4 | 5 | 2 | P |
| Reactive Red Brown H4RReactive Brown - 9 |   | 4 | 5 | 4 | 5 | P |
| Reactive Magenta HBReactive Violet - 13 |   | 4 | 4 | 4 | 1 | F |
| Reactive Purple H3RReactive Violate - 1 |   | 6 | 4 | 5 | 4 | P |
| Reactive Black HNReactive Black - 8 |   | 5 | 4 | 5 | 4 | P |
| Reactive Blue H5RReactive Blue - 13 |   | 5 | 5 | 5 | 1 | P |
| Reactive Blue H2R  |   | 4 | 4 | 4 | 2 | P |
| Reactive Blue H3RPReactive Blue - 49 |   | 4 | 5 | 4 | 2 | P |
| Reactive Tur. Blue H5GReactive Blue - 25 |   | 5-6 | 4-5 | 3 | 3-4 | P |
| Reactive Navy Blue RXReactive Blue - 59 |   | 3 | 3-4 | 4-5 | 1 | P |