RECATIVE HOT DYES

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| **Reactive Hot Dyes** | | **FASTNESS PROPERTIES** | | | | |
| Light | Washing | Perspiration | Hypochlorite | Dischargeability |
| Reactive Yellow H7GL Reactive Yellow - 57 |  | 6 | 5 | 5 | 2 | G |
| Reactive Yellow H4G Reactive Yellow - 18 |  | 6 | 5 | 5 | 1 | G |
| Reactive Gol. Yellow HR Reactive Yellow - 12 |  | 6 | 5 | 5 | 3 | F |
| Reactive Orange H2R Reactive Orange - 13 |  | 4 | 5 | 4 | 4 | P |
| Reactive Red H8B Reactive Red - 31 |  | 4 | 4 | 4 | 3 | P |
| Reactive Red 6BX Reactive Red - 76 |  | 4 | 4 | 5 | 2 | P |
| Reactive Red Brown H4R Reactive Brown - 9 |  | 4 | 5 | 4 | 5 | P |
| Reactive Magenta HB Reactive Violet - 13 |  | 4 | 4 | 4 | 1 | F |
| Reactive Purple H3R Reactive Violate - 1 |  | 6 | 4 | 5 | 4 | P |
| Reactive Black HN Reactive Black - 8 |  | 5 | 4 | 5 | 4 | P |
| Reactive Blue H5R Reactive Blue - 13 |  | 5 | 5 | 5 | 1 | P |
| Reactive Blue H2R |  | 4 | 4 | 4 | 2 | P |
| Reactive Blue H3RP Reactive Blue - 49 |  | 4 | 5 | 4 | 2 | P |
| Reactive Tur. Blue H5G Reactive Blue - 25 |  | 5-6 | 4-5 | 3 | 3-4 | P |
| Reactive Navy Blue RX Reactive Blue - 59 |  | 3 | 3-4 | 4-5 | 1 | P |